RTCD135  SERIES　（85℃ 2000H）

●Compliant to the RoHS directive.

●160WV~600WV extra-high voltage.

●85℃ 2000H for inverters.

■Product Specifications

| (unit: mm) | Items | Specifications |
| --- | --- | --- |
|  | Temperature range | -25℃～+85℃ |
|  | Rated voltage | 160～600V.DC |
|  | Capacitance tolerance | ±20% (20℃, 120Hz) |
|  | Leakage current | 0.01CV (μA)or 5mA,whichever is smaller |
|  |  | [C=nominal capacitance (μF),V= rated voltage (V)] |
|  | Dissipation factor | Less than the value specified in the standard products table. |
| ΦD | P | S | T | Cap material |  | Permissible ripple current | As specified in the standard products table. (40℃, 120Hz) |
| 36 | 12.7 | M5×10 | 6.0 | Phenol |  | High-temperature load | After the rated voltage with specified ripple current is applied at 85℃ for 2,000 hours : Capacitance tolerance : ±20% or less of the initial value Dissipation factor : 200% or less of the specified initial value Leakage current : Specified initial value or less |
| 51 | 22.0 | M5×10 | 5.5 | Phenol |  |  |  |
| 64 | 28.6 | M5×10 | 5.5 | Phenol |  |  |  |
| 77 | 32.0 | M5×10 | 4.5 | Phenol |  |  |  |
| 90 | 32.0 | M5×10 | 4.0 | Phenol |  |  |  |
| 101 | 41.5 | M8×17 | 10.0 | Phenol |  | Standard | JIS C 5101-4 |

| Ripple current correction coefficient |  | Part number(Example): RTCD135 400V 10,000μF±20% F case（Φ90mm）product |
| --- | --- | --- |
| Temperature (℃) | 40 | 60 | 70 | 85 |  |  | RTCD135 2G 103 Y F 157 M D 5 Series Voltage Code Capacitance code Mounting style Diameter code Length Cap. tolerance Diameter Terminal Type of screw |
| Coefficient | 1.0 | 0.75 | 0.62 | 0.37 |  |  |  |
| Frequency (Hz) | 50/60 | 120 | 300 | 1K | ≥10K |  |  |
| Coefficient | 0.7 | 1.0 | 1.1 | 1.3 | 1.4 |  |  |

■Standard Products Table

| Rated Voltage Code (V.DC) | Capacitance (μF) | Case size ΦD×L(mm) | tanδ 20℃, 120Hz | Ripple current 40℃, 120Hz (Arms) | ESR(typ.) 20℃, 100Hz (mΩ) | Z max 20℃, 10KHz (mΩ) | Part number |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 160 2C (200) | 3300 | 36×121 | 0.25 | 14.0 | 35 | 35 | RTCD1352C332IA121M |
|  | 3900 | 51×75 | 0.25 | 14.4 | 30 | 28 | RTCD1352C392YC075M |
|  | 4700 | 51×80 | 0.25 | 15.8 | 25 | 25 | RTCD1352C472YC080M |
|  | 5600 | 51×96 | 0.25 | 19.0 | 23 | 23 | RTCD1352C562YC096M |
|  | 6800 | 51×96 | 0.25 | 21.0 | 20 | 22 | RTCD1352C682YC096M |
|  | 8200 | 51×115 | 0.25 | 24.7 | 18 | 19 | RTCD1352C822YC115M |
|  | 10000 | 64×96 | 0.25 | 28.0 | 15 | 16 | RTCD1352C103YD096M |
|  | 12000 | 64×96 | 0.25 | 30.6 | 12 | 15 | RTCD1352C123YD096M |
|  | 15000 | 64×130 | 0.25 | 38.6 | 11 | 12 | RTCD1352C153YD130M |
|  |  | 77×100 | 0.25 | 38.0 | 11 | 12 | RTCD1352C153YE100M |
|  | 18000 | 64×130 | 0.25 | 42.2 | 9 | 11 | RTCD1352C183YD130M |
|  | 22000 | 77×130 | 0.25 | 49.4 | 8 | 8 | RTCD1352C223YE130M |
|  | 27000 | 77×130 | 0.25 | 54.7 | 7 | 8 | RTCD1352C273YE130M |
|  | 33000 | 90×131 | 0.25 | 64.2 | 6 | 7 | RTCD1352C333YF131M |
|  | 39000 | 90×157 | 0.25 | 75.3 | 5 | 7 | RTCD1352C393YF157M |
| 200 2D (250) | 2200 | 36×100 | 0.25 | 10.6 | 43 | 60 | RTCD1352D222IA100M |
|  | 2700 | 36×121 | 0.25 | 12.7 | 31 | 39 | RTCD1352D272IA121M |
|  | 3300 | 51×80 | 0.25 | 13.3 | 29 | 35 | RTCD1352D332YC080M |
|  | 3900 | 51×75 | 0.25 | 14.4 | 26 | 30 | RTCD1352D392YC075M |
|  | 4700 | 51×96 | 0.25 | 17.4 | 25 | 27 | RTCD1352D472YC096M |
|  | 5600 | 51×115 | 0.25 | 20.4 | 23 | 25 | RTCD1352D562YC115M |
|  | 6800 | 51×130 | 0.25 | 23.7 | 19 | 20 | RTCD1352D682YC130M |
|  | 8200 | 64×96 | 0.25 | 25.4 | 15 | 18 | RTCD1352D822YD096M |
|  | 10000 | 64×96 | 0.25 | 28.0 | 14 | 14 | RTCD1352D103YD096M |
|  | 12000 | 77×96 | 0.25 | 32.6 | 12 | 14 | RTCD1352D123YE096M |
|  | 15000 | 77×96 | 0.25 | 39.0 | 10 | 13 | RTCD1352D153YE096M |

| Rated Voltage Code (V.DC) | Capacitance (μF) | Case size ΦD×L(mm) | tanδ 20℃, 120Hz | Ripple current 40℃, 120Hz (Arms) | ESR(typ.) 20℃, 100Hz (mΩ) | Z max 20℃, 10KHz (mΩ) | Part number |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 200 2D (250) | 18000 | 77×130 | 0.25 | 44.6 | 8 | 12 | RTCD1352D183YE130M |
|  | 22000 | 77×155 | 0.25 | 53.0 | 7 | 7 | RTCD1352D223YE155M |
|  | 27000 | 90×131 | 0.25 | 58.2 | 6 | 7 | RTCD1352D273YF131M |
|  | 33000 | 90×157 | 0.25 | 69.0 | 5 | 7 | RTCD1352D333YF157M |
|  | 36000 | 90×157 | 0.25 | 70.8 | 5 | 7 | RTCD1352D363YF157M |
| 250 2E (300) | 1500 | 36×100 | 0.25 | 8.7 | 53 | 50 | RTCD1352E152IA100M |
|  | 1800 | 36×100 | 0.25 | 9.5 | 46 | 44 | RTCD1352E182IA100M |
|  | 2200 | 51×75 | 0.25 | 10.8 | 38 | 40 | RTCD1352E222YC075M |
|  | 2700 | 51×75 | 0.25 | 12.0 | 33 | 36 | RTCD1352E272YC075M |
|  | 3300 | 51×96 | 0.25 | 14.6 | 28 | 35 | RTCD1352E332YC096M |
|  | 3900 | 51×115 | 0.25 | 17.0 | 25 | 30 | RTCD1352E392YC115M |
|  | 4700 | 64×100 | 0.25 | 19.2 | 21 | 23 | RTCD1352E472YD100M |
|  | 5600 | 64×100 | 0.25 | 21.0 | 19 | 21 | RTCD1352E562YD100M |
|  | 6800 | 64×115 | 0.25 | 24.7 | 15 | 18 | RTCD1352E682YD115M |
|  | 8200 | 64×115 | 0.25 | 27.1 | 13 | 16 | RTCD1352E822YD115M |
|  | 10000 | 64×130 | 0.25 | 31.5 | 12 | 14 | RTCD1352E103YD130M |
|  |  | 77×130 | 0.25 | 34.5 | 12 | 14 | RTCD1352E103YE130M |
|  | 12000 | 77×115 | 0.25 | 34.8 | 10 | 11 | RTCD1352E123YE115M |
|  | 15000 | 77×130 | 0.25 | 40.8 | 8 | 11 | RTCD1352E153YE130M |
|  | 18000 | 77×155 | 0.25 | 47.8 | 7 | 10 | RTCD1352E183YE155M |
|  | 22000 | 90×157 | 0.25 | 56.5 | 6 | 8 | RTCD1352E223YF157M |
| 350 2V (400) | 390 | 36x53 | 0.20 | 4.5 | 272 | 296 | RTCD1352V391IA053M |
|  | 470 | 36×83 | 0.20 | 5.8 | 232 | 245 | RTCD1352V471IA083M |
|  | 560 | 36×83 | 0.20 | 6.4 | 194 | 222 | RTCD1352V561IA083M |
|  | 680 | 36×83 | 0.20 | 7.0 | 156 | 197 | RTCD1352V681IA083M |
|  | 820 | 36×100 | 0.20 | 8.3 | 130 | 174 | RTCD1352V821IA100M |
|  | 1000 | 36×100 | 0.20 | 9.2 | 109 | 135 | RTCD1352V102IA100M |
|  | 1200 | 51×75 | 0.20 | 10.3 | 90 | 120 | RTCD1352V122YC075M |
|  | 1500 | 51×75 | 0.20 | 11.5 | 77 | 100 | RTCD1352V152YC075M |
|  | 1800 | 51×96 | 0.20 | 13.9 | 62 | 80 | RTCD1352V182YC096M |
|  | 2200 | 51×96 | 0.20 | 15.4 | 51 | 70 | RTCD1352V222YC096M |
|  | 2700 | 51×130 | 0.20 | 19.3 | 41 | 58 | RTCD1352V272YC130M |
|  | 3300 | 51×130 | 0.20 | 21.4 | 35 | 51 | RTCD1352V332YC130M |
|  | 3900 | 64×115 | 0.20 | 24.2 | 30 | 47 | RTCD1352V392YD115M |
|  | 4700 | 64×130 | 0.20 | 27.9 | 28 | 40 | RTCD1352V472YD130M |
|  | 5600 | 77×115 | 0.20 | 30.7 | 25 | 35 | RTCD1352V562YE115M |
|  | 6800 | 77×130 | 0.20 | 35.4 | 20 | 29 | RTCD1352V682YE130M |
|  | 8200 | 77×155 | 0.20 | 41.7 | 17 | 25 | RTCD1352V822YE155M |
|  | 10000 | 77×170 | 0.20 | 45.8 | 15 | 23 | RTCD1352V103YE170M |
|  |  | 90×157 | 0.20 | 49.0 | 15 | 23 | RTCD1352V103YF157M |
|  | 12000 | 90×157 | 0.20 | 54.1 | 13 | 21 | RTCD1352V123YF157M |
|  | 15000 | 90×196 | 0.20 | 66.2 | 10 | 20 | RTCD1352V153YF196M |
|  | 18000 | 90×220 | 0.20 | 75.4 | 8 | 20 | RTCD1352V183YF220M |
|  | 22000 | 90×236 | 0.20 | 80.9 | 8 | 20 | RTCD1352V223YF236M |
| 400 2G (450) | 330 | 36×53 | 0.20 | 4.1 | 253 | 440 | RTCD1352G331IA053M |
|  | 390 | 36×83 | 0.20 | 5.3 | 210 | 372 | RTCD1352G391IA083M |
|  | 470 | 36×83 | 0.20 | 5.8 | 181 | 310 | RTCD1352G471IA083M |
|  | 560 | 36×83 | 0.20 | 6.4 | 148 | 260 | RTCD1352G561IA083M |
|  | 680 | 36×100 | 0.20 | 7.6 | 122 | 214 | RTCD1352G681IA100M |
|  | 820 | 36×100 | 0.20 | 8.3 | 101 | 177 | RTCD1352G821IA100M |
|  | 1000 | 51×75 | 0.20 | 9.4 | 85 | 150 | RTCD1352G102YC075M |
|  | 1200 | 51×80 | 0.20 | 10.3 | 75 | 125 | RTCD1352G122YC080M |
|  | 1500 | 51×96 | 0.20 | 12.7 | 62 | 108 | RTCD1352G152YC096M |
|  | 1800 | 51×96 | 0.20 | 13.9 | 51 | 90 | RTCD1352G182YC096M |
|  | 2200 | 51×130 | 0.20 | 17.4 | 39 | 75 | RTCD1352G222YC130M |
|  | 2700 | 64×96 | 0.20 | 18.8 | 36 | 66 | RTCD1352G272YD096M |
|  | 3300 | 64×115 | 0.20 | 22.2 | 35 | 53 | RTCD1352G332YD115M |
|  | 3900 | 64×130 | 0.20 | 25.4 | 29 | 48 | RTCD1352G392YD130M |
|  | 4700 | 77×115 | 0.20 | 28.2 | 26 | 41 | RTCD1352G472YE115M |
|  | 5600 | 77×130 | 0.20 | 32.2 | 21 | 37 | RTCD1352G562YE130M |
|  | 6800 | 77×155 | 0.20 | 38.0 | 18 | 30 | RTCD1352G682YE155M |
|  | 8200 | 90×157 | 0.20 | 44.4 | 16 | 26 | RTCD1352G822YF157M |
|  | 10000 | 90×157 | 0.20 | 49.4 | 13 | 23 | RTCD1352G103YF157M |
|  | 12000 | 90×196 | 0.20 | 59.1 | 12 | 21 | RTCD1352G123YF196M |
|  | 15000 | 90×236 | 0.20 | 71.1 | 10 | 21 | RTCD1352G153YF236M |
| 450 2W (500) | 270 | 36×53 | 0.20 | 3.7 | 422 | 496 | RTCD1352W271IA053M |
|  | 330 | 36×83 | 0.20 | 4.9 | 281 | 406 | RTCD1352W331IA083M |
|  | 390 | 36×83 | 0.20 | 5.3 | 244 | 343 | RTCD1352W391IA083M |
|  | 470 | 36×83 | 0.20 | 5.8 | 201 | 284 | RTCD1352W471IA083M |
|  | 560 | 36×100 | 0.20 | 6.9 | 174 | 238 | RTCD1352W561IA100M |
|  | 680 | 36×100 | 0.20 | 7.6 | 142 | 196 | RTCD1352W681IA100M |
|  | 820 | 51×75 | 0.20 | 8.6 | 99 | 187 | RTCD1352W821YC075M |
|  | 1000 | 51×80 | 0.20 | 9.4 | 84 | 154 | RTCD1352W102YC080M |

| Rated Voltage Code (V.DC) | Capacitance (μF) | Case size ΦD×L(mm) | tanδ 20℃, 120Hz | Ripple current 40℃, 120Hz (Arms) | ESR(typ.) 20℃, 100Hz (mΩ) | Z max 20℃, 10KHz (mΩ) | Part number |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 450 2W (500) | 1200 | 51×96 | 0.20 | 11.4 | 73 | 129 | RTCD1352W122YC096M |
|  | 1500 | 51×115 | 0.20 | 13.7 | 60 | 108 | RTCD1352W152YC115M |
|  | 1800 | 51×130 | 0.20 | 15.8 | 48 | 100 | RTCD1352W182YC130M |
|  | 2200 | 64×100 | 0.20 | 17.0 | 35 | 84 | RTCD1352W222YD100M |
|  | 2700 | 64×115 | 0.20 | 20.2 | 35 | 69 | RTCD1352W272YD115M |
|  | 3300 | 64×130 | 0.20 | 23.4 | 32 | 61 | RTCD1352W332YD130M |
|  | 3900 | 77×115 | 0.20 | 25.6 | 32 | 51 | RTCD1352W392YE115M |
|  | 4700 | 77×130 | 0.20 | 29.4 | 26 | 43 | RTCD1352W472YE130M |
|  | 5600 | 77×155 | 0.20 | 34.6 | 18 | 37 | RTCD1352W562YE155M |
|  | 6800 | 90×157 | 0.20 | 40.5 | 16 | 33 | RTCD1352W682YF157M |
|  | 8200 | 90×157 | 0.20 | 44.6 | 14 | 30 | RTCD1352W822YF157M |
|  | 10000 | 90×196 | 0.20 | 53.9 | 12 | 25 | RTCD1352W103YF196M |
|  | 12000 | 90×236 | 0.20 | 63.8 | 10 | 22 | RTCD1352W123YF236M |
| 500 2H (550) | 1200 | 51x115 | 0.20 | 17.0 | 112 | 120 | RTCD1352H122YC115M |
|  | 1500 | 51x130 | 0.20 | 19.9 | 90 | 96 | RTCD1352H152YC130M |
|  | 1800 | 64x115 | 0.20 | 22.7 | 75 | 80 | RTCD1352H182YD115M |
|  | 2200 | 64x130 | 0.20 | 26.1 | 61 | 65 | RTCD1352H222YD130M |
|  | 2700 | 77x115 | 0.20 | 29.0 | 50 | 53 | RTCD1352H272YE115M |
|  | 3300 | 77x130 | 0.20 | 33.7 | 45 | 48 | RTCD1352H332YE130M |
|  | 3900 | 77x155 | 0.20 | 39.2 | 38 | 41 | RTCD1352H392YE155M |
|  | 4700 | 77x170 | 0.20 | 44.9 | 34 | 37 | RTCD1352H472YE170M |
|  | 5600 | 77x195 | 0.20 | 51.6 | 28 | 31 | RTCD1352H562YE195M |
|  |  | 90x157 | 0.20 | 50.5 | 28 | 31 | RTCD1352H562YF157M |
|  | 6800 | 90x170 | 0.20 | 57.3 | 23 | 25 | RTCD1352H682YF170M |
|  | 8200 | 77x236 | 0.20 | 66.6 | 21 | 23 | RTCD1352H822YE236M |
|  |  | 90x196 | 0.20 | 66.4 | 21 | 23 | RTCD1352H822YF196M |
|  | 10000 | 90x236 | 0.20 | 55.5 | 17 | 19 | RTCD1352H103YF236M |
|  |  | 101x195 | 0.20 | 79.4 | 17 | 19 | RTCD1352H103YG195M |
|  | 12000 | 101x237 | 0.20 | 85.7 | 16 | 18 | RTCD1352H123YG237M |
| 550 2Y (600) | 1000 | 51×130 | 0.20 | 16.2 | 132 | 140 | RTCD1352Y102YC130M |
|  | 1500 | 64×130 | 0.20 | 21.9 | 93 | 100 | RTCD1352Y152YD130M |
|  | 2200 | 77×115 | 0.20 | 25.0 | 65 | 70 | RTCD1352Y222YE115M |
|  | 2700 | 77×130 | 0.20 | 28.9 | 54 | 60 | RTCD1352Y272YE130M |
|  | 3300 | 77×155 | 0.20 | 36.1 | 47 | 50 | RTCD1352Y332YE155M |
|  | 3900 | 77×170 | 0.20 | 43.5 | 40 | 45 | RTCD1352Y392YE170M |
|  | 4700 | 90×145 | 0.20 | 42.6 | 32 | 40 | RTCD1352Y472YF145M |
|  | 5600 | 90×196 | 0.20 | 55.1 | 26 | 30 | RTCD1352Y562YF196M |
|  | 6800 | 90×236 | 0.20 | 65.4 | 21 | 30 | RTCD1352Y682YF236M |
|  | 8200 | 101×237 | 0.20 | 74.0 | 19 | 25 | RTCD1352Y822YG237M |
| 600 2S (650) | 100 | 36×80 | 0.20 | 6.2 | 1582 | 1665 | RTCD1352S101IA080M |
|  | 1200 | 64×96 | 0.20 | 21.1 | 151 | 160 | RTCD1352S122YD096M |
|  | 1500 | 64×115 | 0.20 | 25.4 | 135 | 140 | RTCD1352S152YD115M |
|  | 2200 | 77×115 | 0.20 | 32.7 | 102 | 105 | RTCD1352S222YE115M |
|  | 2700 | 77×130 | 0.20 | 33.0 | 83 | 86 | RTCD1352S272YE130M |
|  | 3300 | 77×170 | 0.20 | 46.5 | 58 | 61 | RTCD1352S332YE170M |
|  | 3900 | 77×195 | 0.20 | 53.5 | 49 | 52 | RTCD1352S392YE195M |
|  | 4700 | 90×157 | 0.20 | 57.0 | 41 | 43 | RTCD1352S472YF157M |