RTCD139  SERIES　　　（ 105℃ 10,000H）

●Compliant to the RoHS directive.

●Long-life series with the warranty of 10,000 hours.

●high-ripple series.

■Specification

| Item | Performance Characteristics |
| --- | --- |
| Operating range | -25℃～+105℃ |
| Rated voltage range | 350V～500V |
| Capacitance tolerance | ±20% (20℃, 120Hz) |
| Leakage current | ≤0.01CV(μA) or 5mA (Whichever is smaller) (20℃, after 5 minutes) C=Nominal capacitance(μF), V=Rated voltage(V) |
| Dissipation factor (20℃，120Hz) | See the standard products table |
| Standard | JIS C 5101-4 |
|  | Useful Life | Load Life | Endurance Test | Shelf Life |
| Lifetime | 15000h | >300000h | 10000h | 10000h | 1000h |
| Leakage Current | Not more than specified value | Not more than specified value | Not more than specified value | Not more than specified value |
| Capacitance Change | Within土30％ of initial value | Within土20％ of initial value | Within土20％ of initial value | Within土20％ of initial value |
| Dissipation Factor | Not more than 300％ of specified value | Not more than 200％ of specified value | Not more than 200％ of specified value | Not more than 200％ of specified value |
| Condition： Applied Voltage Applied Current Applied Temperature Failure Rate Level | UR IR 105℃ ≤1%Failure Rate | UR 1.2×IR 40℃ ≤1%Failure Rate | UR IR 105℃ Guaranteed | UR IR＝0 105℃ | UR＝0 IR＝0 105℃ |

■Drawing                     Unit：mm                               ■Lifetime Diagram

| ΦD | P | S | T | material |  | ΦD | P | S | T | material | 105℃ Multiplier of useful life as a function of ambient temperature and ripple current load ＩＡ：actual ripple current at 120Hz,IR:rated ripple current at 120Hz |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 35 | 12.7 | M5×10 | 6.0 | Phenol |  | 77 | 32.0 | M5×10 | 4.5 | Phenol |  |
| 51 | 22.0 | M5×10 | 5.5 | Phenol |  | 90 | 32.0 | M5×10 | 4.0 | Phenol |  |
| 64 | 28.6 | M5×10 | 5.5 | Phenol |  | 101 | 41.5 | M8×17 | 10.0 | Phenol |  |

| ■Part number(Example)：RTCD139 400V 10,000μF±20% F case（Φ90mm）product |  | ■Ripple current correction coefficient |
| --- | --- | --- |
| RTCD139 2G 103 Y F 196 M D 5 Series Voltage Code Capacitance code Mounting style Diameter code Length Cap. tolerance Diameter Terminal Type of screw |  | T (℃） | 40 | 60 | 85 | 105 |  |
|  |  | Coefficient | 2.44 | 2.16 | 2.0 | 1.0 |  |
|  |  | Frequency (Hz) | 50/60 | 120 | 300 | 1K | ≥10K |
|  |  | Coefficient | 0.7 | 1.0 | 1.1 | 1.24 | 1.3 |

■Standard Products Table

| Rated Voltage Code (V.DC) | Capacitance (μF) | Case size ΦD×L(mm) | tanδ 20℃, 120Hz | Ripple current 40℃, 120Hz (Arms) | ESR(typ.) 20℃, 100Hz (mΩ) | Z max 20℃, 10KHz (mΩ) | Part number |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 350 2V (400) | 2700 | 64×115 | 0.15 | 5.0 | 50 | 55 | RTCD1392V272YD100M |
|  | 3300 | 64×130 | 0.15 | 6.0 | 40 | 45 | RTCD1392V332YD115M |
|  | 3900 | 64×155 | 0.15 | 6.7 | 30 | 35 | RTCD1392V392YD131M |
|  | 4700 | 77×130 | 0.15 | 7.5 | 27 | 30 | RTCD1392V472YE130M |
|  | 5600 | 90×130 | 0.15 | 8.4 | 23 | 25 | RTCD1392V562YF130M |
|  | 6800 | 90×157 | 0.15 | 10.2 | 20 | 23 | RTCD1392V682YF157M |
|  | 8200 | 90×196 | 0.15 | 11.6 | 18 | 21 | RTCD1392V822YF196M |
|  | 10000 | 90×210 | 0.15 | 13.8 | 15 | 18 | RTCD1392V103YF210M |
| 400 2G (450) | 2200 | 64×115 | 0.15 | 5.7 | 48 | 52 | RTCD1392G222YD100M |
|  | 2700 | 64×130 | 0.15 | 6.4 | 40 | 46 | RTCD1392G272YD115M |
|  | 3300 | 64×155 | 0.15 | 7.1 | 35 | 40 | RTCD1392G332YD130M |
|  | 3900 | 77×130 | 0.15 | 8.1 | 30 | 35 | RTCD1392G392YE120M |
|  | 4700 | 77×155 | 0.15 | 9.8 | 25 | 30 | RTCD1392G472YE137M |
|  | 5600 | 90×140 | 0.15 | 10.9 | 20 | 25 | RTCD1392G562YF140M |
|  | 6800 | 90×196 | 0.15 | 13.2 | 16 | 20 | RTCD1392G682YF196M |
|  | 8200 | 90×210 | 0.15 | 15.6 | 13 | 18 | RTCD1392G822YF210M |
| 450 2W (500) | 1800 | 64×115 | 0.15 | 5.5 | 45 | 50 | RTCD1392W182YD100M |
|  | 2200 | 64×130 | 0.15 | 6.3 | 38 | 40 | RTCD1392W222YD130M |
|  | 2700 | 64×155 | 0.15 | 6.9 | 30 | 35 | RTCD1392W272YD155M |
|  | 3300 | 77×130 | 0.15 | 7.8 | 25 | 30 | RTCD1392W332YE130M |
|  | 3900 | 77×155 | 0.15 | 9.5 | 20 | 25 | RTCD1392W392YE155M |
|  | 4700 | 90×157 | 0.15 | 10.7 | 17 | 20 | RTCD1392W472YF157M |
|  | 5600 | 90×196 | 0.15 | 12.3 | 15 | 18 | RTCD1392W562YF196M |
|  | 6800 | 90×210 | 0.15 | 14.8 | 13 | 15 | RTCD1392W682YF210M |
| 500 2H (550) | 1800 | 64×130 | 0.15 | 6.5 | 80 | 95 | RTCD1392H182YD130M |
|  | 2200 | 64×155 | 0.15 | 7.1 | 70 | 80 | RTCD1392H222YD155M |
|  | 2700 | 77×155 | 0.15 | 8.0 | 60 | 70 | RTCD1392H272YE155M |
|  | 3300 | 90×130 | 0.15 | 9.9 | 50 | 61 | RTCD1392H332YF130M |
|  | 3900 | 90×157 | 0.15 | 11.3 | 40 | 49 | RTCD1392H392YF157M |
|  | 4700 | 90×196 | 0.15 | 11.9 | 30 | 42 | RTCD1392H472YF196M |
|  | 5600 | 90×210 | 0.15 | 13.8 | 28 | 30 | RTCD1392H562YF210M |

# Text boxes

After test：

UR to be applied for 60min >24h before measurement